ZHE JIANG WUMEI BIOTECHNOLOGY  CO.,LTD

Tel: +86-579-88230027                           Fax: +86-579-88230028

Email: sales@wumeichem.com                     http: www. wumeichem.com

Add:zhejiang lanxi economic development zone in qiu ling road no.76

Ethylhexyl Palmitate

Manufactured Date: 2018-03-02          Analysis Date: 2018-03-05

Country of Origin: China             CAS No.: 1341-38-4

Specification:

| Item | Specifications | Analysis Results |
| --- | --- | --- |
| Appearance | A colorless or slightly yellow oily liquid | Qualified |
| Content% | ≥98 | 98.70 |
| Color(Hazen) | ≤25 | 15 |
| Acid value（mg KOH/g） | ≤0.5 | 0.10 |
| Density(d425) | 0.840-0.870 | 0.854 |
| Saponification Value mg(KOH)/g | 150～160 | 155 |
| Refractive Index(nD25) | 1.443-1.447 | 1.446 |

Property and Application:

It is a Colorless transparent liquid, and can mix with organic solvent, but not in water. It has no stimulation and allergy to skin. It is not easy to be oxygenated and acetified.It is one of important additives of top grade cosmetics, and it owns excellent performance of infiltration, moistening and softening to skin, so it can be used as emulsifier and wetting agent of cosmetics.

Packing Specification:175kg/Barrel