ZHE JIANG WUMEI BIOTECHNOLOGY  CO.,LTD

Tel: +86-579-88230027                           Fax: +86-579-88230028

Email: sales@wumeichem.com                     http: www. wumeichem.com

Add:zhejiang lanxi economic development zone in qiu ling road no.76

Vaseline

Manufactured Date: 2018-03-11         Analysis Date: 2018-03-19

Country of Origin: China             CAS No.: 8009-03-8

Specification:

| Items | Guideline | Result |
| --- | --- | --- |
| Properties Appearance | Yellow Odorless and non uniform block ointment,should be a certain degree of drawing | PASS |
| Dropping point℃ | 45-60 | 56.50 |
| UV absorbance(290mm)＞ | 0.5 | 0.3 |
| Organic acids mgNaCH/g | 0.08 | 0.06 |
| Degree of acidity andalkalinity | 无 NO | PASS |
| Heterosexual organics | 无 NO | PASS |
| Taper degree (150g25℃)0.1mn | 130-230 | 168 |

Property and Application:

It is a White oily Solid, and can mix with organic solvent, but not in water. It has no stimulation and allergy to skin. It is not easy to be oxygenated and acetified.

It is one of important additives of top grade cosmetics, and it owns excellent performance of infiltration, moistening and softening to skin, so it can be used as emulsifier and wetting agent of cosmetics.

Packing Specification:170kg/165kg/Metal Barrel